1	Abstract

Soils may be categorized into different groups according to their physical properties and it is especially important for civil engineers to understand these properties before the building of any structure. This experiment introduces the concept of Index Properties of Soils as part of classification.  Tests are conducted on the soil samples to analyze their mechanical properties.  Tests such as the Sieve Analysis, Sedimentation Analysis and Atterberg’s Limits test are performed on the soil samples to find out the particle size distribution, Atterberg’s Limits and its moisture content.  By knowing these index properties of the soils, we can understand and predict their behavior in our engineering projects.

2	Acknowledgement

I would like to express my gratitude to Professor Karu who patiently provided us with the detailed background information for the experiment. I would also like to thank Mr. Heng Zee Meng for his guidance and assistance throughout the experiment. Without them, the experiment would not have been so interesting, and this report could not be made possible.

# 3	Aim

This experiment aims to find out the following properties of the soil sample provided.

- Particle size distribution [Size of soil particle and amount in each size].

- Moisture content [Amount of water in a unit dry soil mass].

- Atterberg’s Limits [Plastic Limit and Liquid Limit].

4	Equipment or Apparatus

The following is a list of essential equipment and apparatus used in this experiment.

- Standard sieves of various sizes.

- Hydrometer.

- Measuring cylinder.

- Cone penetrometer.

- Thermometer.

- Weighing machine.

- Oven.

- Dispersing agent (2g/litre of sodium hexametaphosphate).

5	Observations & Results

## 5.1	Particle Size Distribution of Sand

By Sieve Analysis, 200.8 g of sand was passed through a series of standard sieves and a summary of the results is tabulated below in Figure 1.

| Sieve Opening | Weight of Sieve (g) | Weight of Sieve + Dry Soil (g) | Weight of Soil Retained (g) | Percentage Retained (%) | Cumulative Percentage Retained (%) | Percentage Finer (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 1.18 mm | 394.4 | 395.1 | 0.7 | 0.35 | 0.35 | 99.65 |
| 600 m | 336.3 | 401.1 | 64.8 | 32.27 | 32.62 | 67.38 |
| 425 m | 329.3 | 416.8 | 87.5 | 43.57 | 76.19 | 23.81 |
| 300 m | 313.5 | 345.3 | 31.8 | 15.84 | 92.03 | 7.97 |
| 212 m | 308.8 | 318.9 | 10.1 | 5.03 | 97.06 | 2.94 |
| 150 m | 289.6 | 293.6 | 4.0 | 1.99 | 99.05 | 0.95 |
| 63 m | 291.2 | 293.0 | 1.8 | 0.90 | 99.95 | 0.05 |
| Pan | 272.5 | 272.6 | 0.1 | 0.05 | 100.00 | 0.00 |
|  |  |  | 200.8 | 100.00 |  |  |

Figure 1. Particle Size Distribution of Sand by Sieve Analysis

According to the data obtained above, the following proportions of the various particle sizes may be calculated. The grading curve for this sand sample can be found in Appendix A, Figure A1.

- Coarse Sand (600 m to 2000 m)	=	100 - 67.38	=	32.62 %

- Medium Sand (212 m to 600 m)	=	67.38 - 2.94	=	64.44 %

- Fine Sand (63 m to 212 m)		=	2.94 - 0.05	=	2.89 %

- Silt & Clay (< 63 m)			=	0.05 %

It can be observed that the soil consists of mostly medium grain sand particles.  Using the British Soil Classification System (BS 5390: 1981), the soil sample is classified as a Well Graded Sand (SW).

5.2	Particle Size Distribution of Marine Clay

By Sieve Analysis and Sedimentation, 30 g of marine clay was passed through a series of standard sieves and the results are tabulated on the next page in Figure 2.

The grading curve for this marine clay sample can be found as Appendix A, Figure A2. Detailed tabulation of the Sedimentation Analysis results may be found in Appendix B.

| By Sieve Analysis |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Sieve Opening | Weight of Sieve (g) | Weight of Sieve + Dry Soil (g) | Weight of Soil Retained (g) | Percentage Retained (%) | Cumulative Percentage Retained (%) | Percentage Finer (%) |
| 1.18 mm | 131.8 | 131.9 | 0.1 | 0.33 | 0.33 | 99.67 |
| 600 m | 122.7 | 122.8 | 0.1 | 0.33 | 0.66 | 99.34 |
| 425 m | 123.1 | 123.3 | 0.2 | 0.67 | 1.33 | 98.67 |
| 300 m | 115.4 | 115.4 | 0.0 | 0.00 | 1.33 | 98.67 |
| 212 m | 119.1 | 119.3 | 0.2 | 0.67 | 2.00 | 98.00 |
| 150 m | 110.8 | 110.9 | 0.1 | 0.33 | 2.33 | 97.67 |
| 63 m | 115.4 | 115.4 | 0.0 | 0.00 | 2.33 | 97.67 |
| Pan | 85.0 | 85.0 | 0.0 | 0.00 | 2.33 | 97.67 |
| By Sedimentation Analysis |  |  |  |  |  |  |
| Particle Size, D | Elapsed time, t (min) | Reading, Rh' | Rh' + Cm = Rh | Effective Depth, Hr mm | Rh' - Ro' = Rd | Percentage Finer, K (%) |
| 68.5 m | 0.5 | 18.75 | 19.00 | 142 | 18.00 | 96.36 |
| 48.6 m | 1 | 18.50 | 18.75 | 143 | 17.75 | 95.03 |
| 34.4 m | 2 | 18.50 | 18.75 | 143 | 17.75 | 95.03 |
| 24.3 m | 4 | 18.50 | 18.75 | 143 | 17.75 | 95.03 |
| 17.2 m | 8 | 18.50 | 18.75 | 143 | 17.75 | 95.03 |
| 12.6 m | 15 | 18 | 18.25 | 145 | 17.25 | 92.35 |
| 9.1 m | 30 | 17 | 17.25 | 149 | 16.25 | 86.99 |
| 6.5 m | 60 | 16 | 16.25 | 153 | 15.25 | 81.64 |
| 4.3 m | 145 | 14.5 | 14.75 | 159 | 13.75 | 73.61 |
| 3.1 m | 275 | 13.5 | 13.75 | 163 | 12.75 | 68.26 |
| 1.5 m | 1205 | 11.5 | 11.75 | 171 | 10.75 | 57.55 |
| 0.8 m | 4200 | 9.75 | 10.00 | 178 | 9.00 | 48.18 |

Figure 2. Particle Size Distribution of Marine Clay

by Sieve Analysis and Sedimentation Analysis

According to the data obtained above, the following proportions of the various particle sizes may be calculated.

- Coarse Sand (600 m to 2000 m)	=	100 - 99.34	=	0.66 %

- Medium Sand (212 m to 600 m)	=	99.34 - 98.00	=	1.34 %

- Fine Sand (63 m to 212 m)		=	98.00 - 97.67	=	0.33 %

- Coarse Silt (24.3 m to 63 m)		=	97.67 - 95.03	=	2.64 %

- Medium Silt (6.5 m to 24.3 m)		=	95.03 - 81.64	=	13.39 %

- Fine Silt (< 6.5 m)			=	81.64 %

It can be observed that the soil is gap-graded and consists of mostly fine silt particles. Since there is no information about its liquid limit, the soil is classified as Silty Clay.

5.3	Atterberg's Limit of Marine Clay

5.3.1	Liquid Limit

The results of the cone penetration test is tabulated, and the "Average Cone Penetration vs. Moisture Content" graph is plotted in Appendix C.  From the graph, the moisture content of Marine Clay at a 20mm penetration of cone is 74%.

Thus, Liquid Limit of Marine Clay	=	74

    - Plastic Limit

Figure 3 shows a summary of the moisture content of Marine Clay in the Plastic Limit test. Detailed results are shown in Appendix C.

| Set | 1 | 2 | 3 |
| --- | --- | --- | --- |
| Moisture Content (%) | 25.4 | 31.5 | 33.9 |

Figure 3. Moisture Content of Marine Clay by Plastic Limit

Average Moisture Content	=	(25.4 + 31.5 + 33.9) / 3

=	30.3 %

Thus, Plastic Limit of Marine Clay	=	30.3.

Plasticity Index of the Marine Clay 	=	Liquid Limit  - Plastic Limit

=	74 - 30.3

=	43.7

Under the British Soil Classification System (BS 5390: 1981), the marine clay sample is classified as Clay of Very High Plasticity (CV).

6	Discussion

6.1	Sieve Analysis

6.1.1	Sieve analysis is used to determine the particle size distribution for particles larger than 63m.

6.1.2	Errors may have occurred when small particles stick together, especially when the sieve size is small (e.g. 63m) and surface area to volume ratio is so high that attraction due to static forces becomes significant.  This causes sieve analysis results which do not accurately reflect the actual particle sizes. The sand could have been shaken for much longer period to overcome this problem.

6.1.3	Sieve analysis cannot be used for soils with particles smaller than 63m as it is not industrially possible to manufacture finer sieves.

6.1.4	If not for the possible errors discussed above, the sieve analysis is a simple and effective test for investigating the particle size distribution.

6.2	Sedimentation Analysis

6.2.1	Sedimentation analysis is used to determine the particle size distribution for particles smaller than 63m.

6.2.2	The process is time consuming, and requires more calculations and deductions from the data collected in the experiment.

6.2.3	For our experiment on marine clay sample, the sample was passed through a 63m sieve before going through the sieve analysis.  However, our calculations reveal that there are particles with sizes of 68.5 m in the sieve analysis sample.  Therefore, some error must have occurred. Possible errors are as below.

6.2.4	There may be parallax error in taking the readings of the level of the meniscus from the hydrometer.

6.2.5	The small temperature fluctuations of 24.5oC to 25oC will cause a variation in the viscosity of water, but we have assumed a viscosity of 0.891mPa.s for all our calculations.  In fact, a difference of 5oC means a difference of 0.1mPas in viscosity:

| Temperature | Viscosity of Water |
| --- | --- |
| 20 degrees | 1.005 mPa.s |
| 25 degrees | 0.891 mPa.s |
| 30 degrees | 0.801 mPa.s |

6.2.6	The formula used (Stoke’s Law) assumes that the soil particles are spherical, but in reality, particle shapes vary.

6.3	Liquid Limit Test

6.3.1	The water content may not be the same in all parts of the soil because of uneven mixing of water.

6.3.2	The soil may not be placed properly into the metal container, thus trapping air within the sample, resulting in an inaccurate amount of cone penetration.

6.4	Plastic Limit Test

6.4.1	To determine the plastic limit, the soil has to be rolled and re-rolled repeatedly to a diameter of 3 mm until visible cracking occurs.  It is difficult to detect the exact point of the plastic limit because of uneven drying of the sample.  The process will be more effective if a machine is used for this process instead of using one's hands.

6.5	Physical Properties of Soil

6.5.1	The results obtained in the tests in this experiment are useful in determining the physical properties of soil, and they help to determine the way engineering projects are being carried out.

6.5.2	For structures using soils that consist of a higher proportion of silt and clay, a larger footing will be required, as the soil will have lower bearing capacity.

6.5.3	Cohesive soils will less likely be compressed, and soils like the marine clay that consists mainly of fines will be highly compressible.  Therefore, sand, and not clay, is used in concrete columns.

6.5.4	Coarse grain soils are more permeable than fine grain soils such as kaolin clay, and the stability of slopes and embankments are more likely to be affected.  However, fine grain soils have greater frictional resistance because of a greater contact area between particles.  Therefore they will have a higher shear strength.

# 7	Conclusion

From the experiment conducted, it is found that the sand sample is a Well Graded Sand. It consists of mainly medium sand particle of sizes between 212 m to 600 m. The marine clay is gap-graded at the 'medium sand' to 'coarse silt' region. It also consists of mainly fine silt of sizes less than 6 m and has a liquid limit of 74, making it a Clay of Very High Plasticity.

By knowing the properties of the various soils, we are able to apply the knowledge to our engineering applications so that relevant predictions and design decisions may be made.

8	References

  - Geotechnical Engineering - Soil Mechanics

John N. Cernica

John Wiley & Sons Inc., USA

452 pages

  - Essentials of Geology - Fifth Edition

Frederick K. Lutgens and Edward J. Tarbuck

Prentice Hall Inc., USA

480 pages

  - Mechanics of Fluids - Second Edition

Merle C. Potter and David C. Wiggert

Prentice-Hall Inc., USA

749 pages