# Appendix

# Undrained Triaxial Test

# Test 1 - 100 kPa

Diameter of ring/soil 	= 3.8 cm

Height of ring/soil 	= 7.6 cm

Ring + wet soil 		= 618.1 g

Ring only 		= 474.6 g

Wet soil only 		= 143.5 g

Volume of soil 		= 86.193 cm3

Bulk density 		= 1.665 g/cm3

## Water Content

|  | Before loading |  |  | After loading |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Can No. | 1 | 2 | 3 | 1 | 2 | 3 |
| Can + wet (g) | 12.7 | 19.2 | 12.7 | 30.4 | 30.7 | 41.3 |
| Can + dry (g) | 9.3 | 13.5 | 9.6 | 20.1 | 20.0 | 27.3 |
| Can only (g) | 5.3 | 5.6 | 5.0 | 3.2 | 3.2 | 5.3 |
| Water (g) | 3.4 | 5.7 | 3.1 | 10.3 | 10.7 | 14.0 |
| Dry soil (g) | 4.0 | 7.9 | 4.6 | 16.9 | 16.8 | 22.0 |
| Water content (%) | 85.00 | 72.15 | 67.39 | 60.95 | 63.69 | 63.64 |
| w (%) |  |  |  |  |  | 68.80 |

## Triaxial Test Results

| Comp Gauge Reading (div) | Force Gauge Reading (div) | Comp of Sample Del L (mm) | Strain E (%) L = 76mm | Corrected Area A (mm2) D = 38 mm | Deviator Force P (N) | Deviator Stresses P/A (kPa) |
| --- | --- | --- | --- | --- | --- | --- |
| 0 | 18.5 | 0 | 0 | 1134.3 | 0 | 0 |
| 50 | 22.0 | 0.5 | 0.66 | 1141.7 | 4.700 | 4.116 |
| 100 | 23.5 | 1.0 | 1.32 | 1149.4 | 6.714 | 5.841 |
| 150 | 24.0 | 1.5 | 1.97 | 1157.1 | 7.385 | 6.383 |
| 200 | 25.0 | 2.0 | 2.63 | 1164.9 | 8.728 | 7.493 |
| 250 | 26.0 | 2.5 | 3.29 | 1172.8 | 10.071 | 8.587 |
| 300 | 26.5 | 3.0 | 3.94 | 1180.8 | 10.742 | 9.098 |
| 400 | 28.0 | 4.0 | 5.25 | 1197.3 | 12.757 | 10.654 |
| 500 | 28.5 | 5.0 | 6.58 | 1214.1 | 13.428 | 11.060 |
| 600 | 28.5 | 6.0 | 7.89 | 1231.5 | 13.428 | 10.904 |
| 700 | 29.0 | 7.0 | 9.21 | 1249.3 | 14.099 | 11.286 |
| 800 | 29.5 | 8.0 | 10.52 | 1267.7 | 14.771 | 11.652 |
| 900 | 30.0 | 9.0 | 11.84 | 1286.6 | 15.442 | 12.002 |
| 1000 | 30.0 | 10.0 | 13.16 | 1306.1 | 15.442 | 11.823 |
| 1100 | 30.0 | 11.0 | 14.47 | 1326.2 | 15.442 | 11.644 |
| 1200 | 30.5 | 12.0 | 15.78 | 1346.9 | 16.114 | 11.963 |
| 1300 | 31.0 | 13.0 | 17.10 | 1386.3 | 16.785 | 12.108 |
| 1400 | 31.5 | 14.0 | 18.42 | 1390.4 | 17.456 | 12.555 |
| 1500 | 31.5 | 15.0 | 19.74 | 1413.3 | 17.456 | 12.352 |

### By Wood’s Correlation,

LI	=	(w-PL)/PI	= 0.8810

# Cu 	= 	170e(-4.6LI)	= 2.954 kPa

# From the Graph of Deviator Stress vs Axial Strain,

### At maximum point,

### Strain 				= 18.42 %

### Deviator Stress 		= 12.555 kPa

From the Membrane Correction Graph,

### Membrane correction 		= 1.818 kPa

Corrected Deviator Stress	= 12.555 – 1.818 = 10.737 kPa

1 = 100kPa

3 = 100 + 10.737 = 110.737 kPa

# Test 2 - 200 kPa

Diameter of ring/soil 	= 3.8 cm

### Height of ring/soil 	= 7.6 cm

Ring + wet soil 		= 611.0 g

Ring only 			= 472.1 g

Wet soil only 			= 138.9 g

Volume of soil 		= 86.193 cm3

Bulk density 			= 1.612 g/cm3

# Water Content

|  | Before loading |  |  | After loading |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Can No. | 1 | 2 | 3 | 1 | 2 | 3 |
| Can + wet (g) | 20.1 | 25.0 | 19.8 | 28.8 | 34.3 | 32.6 |
| Can + dry (g) | 13.2 | 17.1 | 13.0 | 18.7 | 22.2 | 23.3 |
| Can only (g) | 3.2 | 5.4 | 3.1 | 3.4 | 3.4 | 9.1 |
| Water (g) | 6.9 | 7.9 | 6.8 | 10.1 | 12.1 | 9.3 |
| Dry soil (g) | 10.0 | 11.7 | 9.9 | 15.3 | 18.8 | 14.2 |
| Water content (%) | 69.00 | 67.52 | 68.69 | 66.01 | 64.36 | 65.49 |
| w (%) |  |  |  |  |  | 66.85 |

# Triaxial Test Results

| Comp Gauge Reading (div) | Force Gauge Reading (div) | Comp of Sample Del L (mm) | Strain E (%) L = 76mm | Corrected Area A (mm2) D = 38 mm | Deviator Force P (kN) | Deviator Stresses P/A kPa |
| --- | --- | --- | --- | --- | --- | --- |
| 0 | 35.5 | 0 | 0 | 1134.3 | 0 | 0 |
| 50 | 38 | 0.5 | 0.66 | 1141.7 | 3.357 | 2.940 |
| 100 | 40 | 1.0 | 1.32 | 1149.4 | 6.043 | 5.257 |
| 150 | 42 | 1.5 | 1.97 | 1157.1 | 8.728 | 7.543 |
| 200 | 43 | 2.0 | 2.63 | 1164.9 | 10.071 | 8.645 |
| 250 | 44 | 2.5 | 3.29 | 1172.8 | 11.414 | 9.732 |
| 300 | 45 | 3.0 | 3.94 | 1180.8 | 12.757 | 10.803 |
| 400 | 45 | 4.0 | 5.25 | 1197.3 | 12.757 | 10.654 |
| 500 | 45.5 | 5.0 | 6.58 | 1214.1 | 13.428 | 11.060 |
| 600 | 46 | 6.0 | 7.89 | 1231.5 | 14.099 | 11.449 |
| 700 | 47 | 7.0 | 9.21 | 1249.3 | 15.442 | 12.361 |
| 800 | 47 | 8.0 | 10.52 | 1267.7 | 15.442 | 12.181 |
| 900 | 48 | 9.0 | 11.84 | 1286.6 | 16.785 | 13.046 |
| 1000 | 48 | 10.0 | 13.16 | 1306.1 | 16.785 | 12.851 |
| 1100 | 48 | 11.0 | 14.47 | 1326.2 | 16.785 | 12.656 |
| 1200 | 48 | 12.0 | 15.78 | 1346.9 | 16.785 | 12.462 |
| 1300 | 48 | 13.0 | 17.10 | 1386.3 | 16.785 | 12.108 |
| 1400 | 48 | 14.0 | 18.42 | 1390.4 | 16.785 | 12.072 |
| 1500 | 48 | 15.0 | 19.74 | 1413.3 | 16.785 | 11.876 |

### By Wood’s Correlation,

LI	=	(w-PL)/PI	= 0.8364

#### Cu 	= 	170e(-4.6LI)	= 3.627 kPa

# From the Graph of Deviator Stress vs Axial Strain,

### At maximum point,

### Strain 				= 11.84 %

### Deviator Stress 		= 13.046 kPa

From the Membrane Correction Graph,

### Membrane correction 		= 1.318 kPa

Corrected Deviator Stress	= 13.046 – 1.318 = 11.728 kPa

1 = 200kPa

3 = 200 + 11.728 = 211.728 kPa

#### For Undrained Triaxial Test

By Wood’s Correlation,

Average Cu = 3.29 kPa

By measurement,

By drawing the Mohr’s Circle and finding the y-intercept,

Measured Cu = 5 kPa

# Torvane Test

## Test 1

| Can No. | 1 | 2 | 3 |
| --- | --- | --- | --- |
| Can + wet (g) | 35.7 | 33.2 | 30.1 |
| Can + dry (g) | 27.7 | 23.4 | 21.6 |
| Can only (g) | 16.0 | 9.1 | 9.3 |
| Water (g) | 8.0 | 9.8 | 8.5 |
| Dry soil (g) | 11.7 | 14.3 | 12.3 |
| Water content (%) | 68.38 | 68.53 | 69.11 |
| w (%) |  |  | 68.67 |

By Wood’s Correlation,

LI	=	(w-PL)/PI	= 0.8780

Cu 	= 	170e(-4.6LI)	= 2.995 kPa

Test 1 reading 	= 0.08 kg/cm2

### Measured Cu 	= 8.0 kPa

## Test 2

| Can No. | 4 | 5 | 6 |
| --- | --- | --- | --- |
| Can + wet (g) | 21.1 | 25.6 | 25.8 |
| Can + dry (g) | 15.0 | 17.8 | 19.0 |
| Can only (g) | 6.3 | 6.6 | 9.1 |
| Water (g) | 6.1 | 7.8 | 6.8 |
| Dry soil (g) | 8.7 | 11.2 | 9.9 |
| Water content (%) | 70.11 | 69.64 | 68.69 |
| w (%) |  |  | 69.48 |

By Wood’s Correlation,

LI	=	(w-PL)/PI	= 0.8966

Cu 	= 	170e(-4.6LI)	= 2.750 kPa

Test 2 reading 	= 0.07 kg/cm2

Measured Cu 	= 7 kPa

## Test 3

| Can No. | 7 | 8 | 9 |
| --- | --- | --- | --- |
| Can + wet (g) | 20.2 | 22.5 | 24.6 |
| Can + dry (g) | 13.4 | 14.7 | 16.0 |
| Can only (g) | 3.2 | 3.2 | 3.2 |
| Water (g) | 6.8 | 7.8 | 8.6 |
| Dry soil (g) | 10.2 | 11.5 | 12.8 |
| Water content (%) | 66.67 | 67.83 | 67.19 |
| w (%) |  |  | 67.23 |

By Wood’s Correlation,

LI	=	(w-PL)/PI	= 0.8451

Cu 	= 	170e(-4.6LI)	= 3.485 kPa

Test 3 reading 	= 0.1 kg/cm2

Measured Cu 	= 10 kPa

## Test 4

| Can No. | 10 | 11 | 12 |
| --- | --- | --- | --- |
| Can + wet (g) | 24.5 | 26.4 | 21.9 |
| Can + dry (g) | 16.4 | 17.2 | 14.8 |
| Can only (g) | 4.5 | 3.8 | 4.2 |
| Water (g) | 8.1 | 9.2 | 7.1 |
| Dry soil (g) | 11.9 | 13.4 | 10.6 |
| Water content (%) | 68.07 | 68.66 | 66.98 |
| w (%) |  |  | 67.90 |

By Wood’s Correlation,

LI	=	(w-PL)/PI	= 0.8604

Cu 	= 	170e(-4.6LI)	= 3.248 kPa

Test 4 reading 	= 0.1 kg/cm2

Measured Cu	= 10 kPa

#### For Torvane Test

By Wood’s Correlation,

Average Cu = 3.12 kPa

# By measurement,

Average Cu = 8.75 kPa

# Laboratory Vane Test

## Test 1

| Can No. | 1 | 2 | 3 |
| --- | --- | --- | --- |
| Can + wet (g) | 48.8 | 35.9 | 27.6 |
| Can + dry (g) | 32.0 | 23.3 | 19.5 |
| Can only (g) | 6.4 | 4.0 | 6.9 |
| Water (g) | 16.8 | 12.6 | 8.1 |
| Dry soil (g) | 25.6 | 19.3 | 12.6 |
| Water content (%) | 65.63 | 65.28 | 64.29 |
| w (%) |  |  | 65.07 |

By Wood’s Correlation,

LI	=	(w-PL)/PI	= 0.7957

Cu 	= 	170e(-4.6LI)	= 4.375 kPa

Deflection 	= 24.5 o

Measured Cu	= 7.5 kPa

## Test 2

| Can No. | 4 | 5 | 6 |
| --- | --- | --- | --- |
| Can + wet (g) | 21.8 | 23.7 | 19.5 |
| Can + dry (g) | 14.3 | 15.8 | 12.9 |
| Can only (g) | 3.2 | 4.0 | 3.1 |
| Water (g) | 7.5 | 7.9 | 6.6 |
| Dry soil (g) | 11.1 | 11.8 | 9.8 |
| Water content (%) | 67.57 | 66.95 | 67.35 |
| w (%) |  |  | 67.29 |

By Wood’s Correlation,

LI	=	(w-PL)/PI	= 0.8465

Cu 	= 	170e(-4.6LI)	= 3.463 kPa

Deflection 	= 24 o

Measured Cu	= 7.2 kPa

For Laboratory Vane Test

By Wood’s Correlation,

Average Cu = 3.92 kPa

By measurement,

Average Cu = 7.35 kPa

# Cone Penetrometer Test

## Test 1

| Can No. | 1 | 2 | 3 |
| --- | --- | --- | --- |
| Can + wet (g) | 19.9 | 20.4 | 24.8 |
| Can + dry (g) | 14.2 | 14.3 | 17.1 |
| Can only (g) | 6.0 | 6.2 | 6.1 |
| Water (g) | 5.7 | 6.1 | 7.7 |
| Dry soil (g) | 8.2 | 8.1 | 11.0 |
| Water content (%) | 69.51 | 75.31 | 70.00 |
| w (%) |  |  | 71.61 |

By Wood’s Correlation,

LI	=	(w-PL)/PI	= 0.9453

Cu 	= 	170e(-4.6LI)	= 2.198 kPa

Result 1	= 0.4 kg

Measured Cu	= 0.08 kg/m2

= 7.848 kPa

## Test 2

| Can No. | 4 | 5 | 6 |
| --- | --- | --- | --- |
| Can + wet (g) | 20.8 | 25.4 | 30.3 |
| Can + dry (g) | 15.0 | 17.8 | 21.0 |
| Can only (g) | 6.1 | 6.4 | 7.6 |
| Water (g) | 5.8 | 7.6 | 9.3 |
| Dry soil (g) | 8.9 | 11.4 | 13.4 |
| Water content (%) | 65.17 | 66.67 | 69.40 |
| w (%) |  |  | 67.08 |

By Wood’s Correlation,

LI	=	(w-PL)/PI	= 0.8416

Cu 	= 	170e(-4.6LI)	= 3.540 kPa

Result 2	= 0.4 kg

Measured Cu	= 0.08 kg/m2

= 7.848 kPa

## Test 3

| Can No. | 7 | 8 | 9 |
| --- | --- | --- | --- |
| Can + wet (g) | 29.9 | 26.0 | 29.6 |
| Can + dry (g) | 19.5 | 17.0 | 19.5 |
| Can only (g) | 4.2 | 3.5 | 4.7 |
| Water (g) | 10.4 | 9.0 | 10.1 |
| Dry soil (g) | 15.3 | 13.5 | 14.8 |
| Water content (%) | 67.97 | 66.67 | 68.24 |
| w (%) |  |  | 67.63 |

By Wood’s Correlation,

LI	=	(w-PL)/PI	= 0.8542

Cu 	= 	170e(-4.6LI)	= 3.341 kPa

Result 3	= 0.3 kg

Measured Cu 	= 0.075 kg/m2

## = 7.358 kPa

## Test 4

| Can No. | 10 | 11 | 12 |
| --- | --- | --- | --- |
| Can + wet (g) | 31.2 | 26.5 | 29.6 |
| Can + dry (g) | 20.1 | 17.0 | 19.2 |
| Can only (g) | 4.0 | 3.1 | 4.0 |
| Water (g) | 11.1 | 9.5 | 10.4 |
| Dry soil (g) | 16.1 | 13.9 | 15.2 |
| Water content (%) | 68.94 | 68.35 | 68.42 |
| w (%) |  |  | 68.57 |

By Wood’s Correlation,

LI	=	(w-PL)/PI	= 0.8757

Cu 	= 	170e(-4.6LI)	= 3.026 kPa

Result 4	= 0.35 kg

Measured Cu	= 0.077 kg/m2

= 7.554 kPa

For Cone Penetrometer Test

By Wood’s Correlation,

Average Cu = 3.03 kPa

By measurement,

Average Cu = 7.65 kPa